A comprehensive dataset of chloride thresholds and electrochemical parameters for steel rebar corrosion in cementitious environments

Usage Notes for the Dataset:

1. Dataset Overview

This dataset is a centralized, comprehensive collection of chloride threshold values and electrochemical parameters for steel rebar corrosion in cementitious environments, compiled from peer-reviewed published literature and experimental datasets. The dataset includes steel and cementitious-material information, simulated concrete pore-solution composition, CT values, corrosion potential (Ecp), pitting potential (Eb), pH, exposure conditions, and associated source information.

2. File Structure

The repository record contains two files:

A comprehensive dataset of chloride thresholds and electrochemical parameters for steel rebar corrosion in cementitious environments.xlsx

Dataset_Usage_Notes.docx — this document, describing the workbook structure, conventions, provenance, and citation guidance.

- Worksheet Descriptions

This dataset covers relevant articles from the past nearly seven decades. The information and descriptions corresponding to each sheet are as follows:

| Worksheet | Material category | General content |
| --- | --- | --- |
| Sheet1 | Carbon steel 1 | CT, electrochemical, material/environmental, and source data before 2019 |
| Sheet2 | Carbon steel 2 | CT, electrochemical, material/environmental, and source data since 2019 |
| Sheet3 | Stainless steel 1 | CT, electrochemical, material/environmental, and source data before 2019 |
| Sheet4 | Stainless steel 2 | CT, electrochemical, material/environmental, and source data since 2019 |

4. Missing Value Representation

Missing values in the dataset are uniformly and consistently represented by empty cells (None). No special placeholder values are used to denote missing or unmeasured data. Any cell without a numerical or alphanumeric value is defined as a missing entry for that specific parameter.

5. Reference Electrode Conversion for Potential Measurements

All electrochemical potential measurements (including corrosion potential Ecp and pitting potential Epit) in the dataset have been pre-unified and fully converted to the Saturated Calomel Electrode (SCE) scale. All potential-related column headers are explicitly labeled with the unit "Vsce", confirming that values are referenced to the SCE electrode. No additional reference electrode conversion is required for end users.

6. Identification of Digitized Literature Data

Data digitized from published literature images (e.g., electrochemical polarization curves, corrosion potential plots, or chloride threshold charts extracted from peer-reviewed papers) is identified through two primary, consistent markers:

Literature Citation Traceability: All digitized data records include a full citation to the original literature source in the "References" column, linking the digitized value to its published origin.

Special Color Markers: For data marked in red in the sheet, the explanations for the corresponding physical quantities are as follows:

Ecp: Indicates that this value was not obtained from actual measurements in the literature and was not used in subsequent analysis of this database.

Ec: Indicates that this value was calculated rather than obtained from actual measurements in the literature.

pH: Indicates that this value was calculated based on solution composition rather than obtained from actual measurements in the literature.

Density: Indicates the average density of all collected data.

Additional notes on digitization protocols or uncertainty are included in the "Notes and comments" column where available.